**LED-Handrail Profile Emil (40 x 40 x 1,5mm) with ribs**

**Profile grooved tube with ribs in the groove**

Dimensions: Profile ribbed tube 40x40x1,5mm, groove 24x24mm with ribs for directly snapping in the plastic cover.  
Material**:** 1.4301/07 (V2A) – AISI 304  
Surface**:** axially ground grain, similar to K240

Manufactured according to DIN EN ISO 9445 T2, DIN EN 10088.  
Dimensions according to EN 10162 and EN 10021.  
Profile with cold-formed rolled-in groove, longitudinally welded, with weld seam in the groove.  
Batch and material in the groove.Bar length: 6mAcceptance test certificate (Apz.) 3.1 available.