**LED-Handrail Profile Lilly (ø42.4mm x 1.5mm) with ribs**

**Profile grooved tube with ribs in the groove**

Dimensions: Profile ribbed tube ø42.4x1.5mm, groove 24x24mm with ribs for directly snapping in the plastic cover.  
Material**:** 1.4401/04 (V4A) – AISI 316(L)  
Surface**:** Radially ground grain, similar to K240

Manufactured according to DIN EN ISO 9445 T2, DIN EN 10088.  
Dimensions according to EN 10162 and EN 10021.  
Profile with cold-formed rolled-in groove, longitudinally welded, with weld seam in the groove.  
Batch and material in the groove.Bar length: 6mAcceptance test certificate (Apz.) 3.1 available.

Manufacturer:LUX GLENDER GmbH