**LED Handrail Profile Paula (ø48,3 x 1,5mm)**

**Profile tube with groove**

Dimensions: Profile groove tube ø48,3x1,5mm, Nut 27x30mm

Material: 1.4301/07 (V2A) – AISI 304

Surface: Radially ground grain, similar to K240

Manufactured according to DIN EN ISO 9445 T2, DIN EN 10088.

Dimensions according to EN 10162 and EN 10021.

Profile with cold-formed rolled-in groove, longitudinally welded.

Batch and material in the groove.

Bar length: 6m

Acceptance test certificate (Apz.) 3.1 available.

Manufacturer: LUX GLENDER GmbH